Item 514 Structural Steel Painting

| District: | Date: | Project No.: | Co/Rt/Sec: |
| --- | --- | --- | --- |
| Contractor: | Project/District Contacts: |
| Reviewed “√” | Specification Conformance Statement | CMS/ CIM | Measurements | Conformance Comments |
|  | Was the Engineer provided with all the required testing equipment? | 514.04 |  |  |
|  | Was the quality control specialist properly trained? | 514.03 |  |  |
|  | If production work was taking place, was the quality control specialist involved in any other activities not related to quality control? | 514.03 |  |  |
|  | Was the quality control specialist properly equipped? | 514.03 |  |  |
|  | Was the quality control specialist able to climb? | 514.03 |  |  |
|  | Was there a MSDS provided for all abrasives, paints, and thinners? | 514.08 |  |  |
|  | Was the steel temperature at least 5 degrees above dew point before blasting or painting the steel? | 514.05 |  |  |
|  | Were air compressors checked every four hours? | 514.03 |  |  |
|  | Was the thinner from the same manufacture as the paint? | 514.14 |  |  |
|  | Were printed instructions from the manufacture available pertaining to thinning of the paint? | 514.14 |  |  |
|  | Were shear mixers used to mix the paint? | 514.14 |  |  |
|  | Was primer continuously mixed during application? | 514.14 |  |  |
|  | Was relative humidity below 85% during application of paint? | 514.06 B |  |  |
|  | Was proper scaffolding used for inspection? | 514.09 |  |  |
|  | Were the tarps installed correctly? | 514.11D |  |  |
|  | Was all equipment parked on ground covers? | 514.11D |  |  |
|  | Was the debris collected and stored at the end of each day? | 514.11D |  |  |
|  | Was the debris properly stored? | 514.11D |  |  |
|  | Were debris sampled within the first week of production blasting? | 514.11D |  |  |
|  | Was hazardous waste disposed of within 60 days after it was generated? | 514.11D |  |  |
|  | Were all damaged areas properly repaired? | 514.19 |  |  |