2007 Technical Process Review Checklist

Item 252 Full Depth Pavement Removal and Flexible Replacement

| District | Date | Project No. | Co/Rt/Sec. |
| --- | --- | --- | --- |
| Contractor: | Project/District Contacts: |
|  | Review “√” | Specification Conformance Statement | CMS/ CIM | Measurements | Conformance Comments |
| Removal of Existing Pavement |
| 1 |  | Repair areas are marked before the start of diamond sawing. | 252.02 255.03 |  |  |
| 2 |  | Diamond saw blade used for the full depth pavement sawing. | 252.02 255.03 |  |  |
| 3 |  | The lift out method is used for pavement removal. | 252.02 255.03 |  |  |
| 4 |  | Adjacent pavement or shoulder is damaged during the pavement sawing or pavement removal. | 252.02 255.03 |  |  |
| 5 |  | The subgrade/subbase is Shaped and compacted properly. | 252.03255.04 |  |  |
| 6 |  | Transverse joints are trimmed to vertical 1.5 inches minimum | CIM |  |  |
| Placement of Asphalt concrete |
| 7 |  | Surfaces on which the asphalt concrete is to be placed are clean and free of contaminants. | 401.14 |  |  |
| 8 |  | Proper tack coat is used and applied to exposed surfaces. | 401.14 |  |  |
| 9 |  | 301 or 448 asphalt concrete temperature at time of placement. | JMF |  |  |
| 10 |  | 301 or 448 asphalt is used to an elevation that results in pavement flush to the top of pavement. | 252.04 401.16 |  |  |
| 11 |  | 10 foot straight edge is being used. Surface flush + ¼”. |  |  |  |
| 12 |  | Proper compaction was performed. Type I pneumatic tire roller. | 252.04401.13 |  |  |
| 13 |  | Joints perimeters were sealed properly using approved 702.04 Rs-1, RS-2, CRS-1 or CRS-2 | 252.04 702.04 |  |  |
| Documentation(Measurement & Payment) |
| 14 |  | Sawing quantities were measured in feet. | 252.05 252.06 |  |  |
| 15 |  | Areas of repairs measured and converted to square yards by project personnel. | 252.05 252.06 |  |  |
| 16 |  | The location of the repair dimensions and calculations are documented on a CA-D -6. | CIM |  |  |