- 251 Partial Depth Repair

- Description (251.01)

This work consists of partial depth removal of existing pavement in areas exhibiting surface deterioration, applying tack coat, and placing and compacting asphalt concrete.

- Removal of Existing Pavement (251.02)

The Engineer should designate the location and mark the limits of the areas to be repaired.  Unless otherwise specified on the plans, extend repair area transversely the full width of a traffic lane and longitudinally along the longitudinal joint.  Mark the areas in rectangular shapes enveloping the deteriorated surface.   Use aerosol spray paint that should be provided by the contractor.  Ensure pavement is removed to the depth shown on the plans and that adjacent pavement is not damaged.  If the adjacent pavement is damaged, remove all loose pavement to the depth specified on the plans.  The contractor should dispose of removed pavement according to 202.

- Placement of Asphalt Concrete (251.03)

The exposed surfaces must be thoroughly cleaned and coated with 407.02 material to fill all cracks and joint openings.  The approved 448 asphalt concrete must be placed and compacted in as many lifts as necessary to finish flush with the adjacent pavement surface.

Continuously compact each lift while the material is in a workable condition throughout the depth of the lift.

The final lift must be compacted thoroughly using a Type I pneumatic tire roller that conforms to 401.13.  As the rolling progresses, add additional patching material, as necessary, to produce a smooth surface flush with the existing pavement surface.

The contractor should not vary the final lift of each completed section from a testing 10-foot (3 m) straightedge by more than 1/4 inch (6 mm).

Trim to vertical all transverse joints 1.5 inches (38 mm) minimum before placing the final asphalt concrete layer adjacent to the existing pavement, unless the repair area is covered with an overlay of asphalt concrete within 60 days.

If the Contract does not include resurfacing, seal the perimeter surface of the repaired areas 4” (100 mm) wide by applying approved 702.04 asphalt material, RS-1, RS-2, CRS-1, CRS-2, or 702.01 approved binder.

- Documentation Requirements - 251 Partial Depth Pavement Repair

- Mark areas to be repaired in rectangular shapes

- Remove deteriorated pavement to a suitable depth

- Dispose of removed pavement as per 203.01

- Area to be clean and tacked with 407 tack coat

- Place and compact approved 448 Type I asphalt

- Location, measure, and pay per 251.04

- Document on CA-D-6