**Compatibility of Pavement Marking Materials for Restripe Situations**

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Existing (Old) Pavement Marking Material** | **Restripe (New) Pavement Marking Material** | | | | | | |
| Traffic Paint**1** | Polyester**1** | Thermoplastic | Preformed (Item 645) | Epoxy | Heat-Fused Preformed | Spray Thermoplastic |
| Traffic Paint3 | **Y** | **Y** | **Y2** | **N** | **N** | **N** | **Y2** |
| Polyester | **Y** | **Y** | **N** | **N** | **N** | **N** | **N** |
| Thermoplastic | **Y** | **N** | **N** | **N** | **N** | **N** | **Y** |
| Preformed (Item 645) | **N** | **N** | **N** | **N** | **N** | **N** | **N** |
| Epoxy | **Y** | **N** | **N** | **N** | **N** | **N** | **N** |
| Heat-Fused Preformed | **N** | **N** | **N** | **N** | **N** | **N** | **Y** |
| Spray Thermoplastic | **Y** | **N** | **Y** | **N** | **N** | **N** | **Y** |

All pavement marking materials are compatible for striping over Class III Work Zone Markings.

**Notes:**

1. Do not use wet glass beads
2. Apply only if existing marking is at least 3 months old
3. Includes Class I and II Work Zone Markings